PhotoKPFM/PL Supplementary Tables S1-S4

Table S1. Ternary-library photoKPFM experimental acquisition log. Each row is one paired dark and illuminated acquisition stored in the supplied raw HDF5 file. Plate indices are zero-based and are mapped to the included 96-well nominal-composition lookup. Ternary scans contain 128 × 128 pixels over a 5 × 5 µm² area, as stated in the current manuscript Methods. The HDF5 file contains acquisition-order identifiers but no exact clock timestamps or external calibration metadata; neither is inferred here. Surface-potential measurements remain relative, uncalibrated instrument signals.

| Acquisition iteration | Plate index (zero-based) | Well ID | Nominal FAPbI3 (%) | Nominal BDAPbI4 (%) | Nominal PEA2PbI4 (%) | Dark acquisition ID | Illuminated acquisition ID | Scan pixels | Scan area |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | A1 | 0 | 0 | 100 | exp3_0000 | exp3_0001 | 128 × 128 | 5 × 5 µm² |
| 2 | 40 | A6 | 32 | 32 | 36 | exp3_0002 | exp3_0003 | 128 × 128 | 5 × 5 µm² |
| 3 | 78 | G10 | 0 | 96 | 4 | exp3_0004 | exp3_0005 | 128 × 128 | 5 × 5 µm² |
| 4 | 90 | C12 | 96 | 0 | 4 | exp3_0006 | exp3_0007 | 128 × 128 | 5 × 5 µm² |
| 5 | 1 | B1 | 0 | 8 | 92 | exp3_0008 | exp3_0009 | 128 × 128 | 5 × 5 µm² |
| 6 | 45 | F6 | 0 | 72 | 28 | exp3_0010 | exp3_0011 | 128 × 128 | 5 × 5 µm² |
| 7 | 35 | D5 | 56 | 0 | 44 | exp3_0012 | exp3_0013 | 128 × 128 | 5 × 5 µm² |
| 8 | 81 | B11 | 24 | 72 | 4 | exp3_0014 | exp3_0015 | 128 × 128 | 5 × 5 µm² |
| 9 | 87 | H11 | 72 | 24 | 4 | exp3_0016 | exp3_0017 | 128 × 128 | 5 × 5 µm² |
| 10 | 78 | G10 | 0 | 96 | 4 | exp3_0018 | exp3_0019 | 128 × 128 | 5 × 5 µm² |
| 11 | 7 | H1 | 8 | 16 | 76 | exp3_0020 | exp3_0021 | 128 × 128 | 5 × 5 µm² |
| 12 | 0 | A1 | 0 | 0 | 100 | exp3_0022 | exp3_0023 | 128 × 128 | 5 × 5 µm² |
| 13 | 16 | A3 | 8 | 32 | 60 | exp3_0024 | exp3_0025 | 128 × 128 | 5 × 5 µm² |
| 14 | 78 | G10 | 0 | 96 | 4 | exp3_0026 | exp3_0027 | 128 × 128 | 5 × 5 µm² |
| 15 | 0 | A1 | 0 | 0 | 100 | exp3_0028 | exp3_0029 | 128 × 128 | 5 × 5 µm² |
| 16 | 46 | G6 | 8 | 64 | 28 | exp3_0030 | exp3_0031 | 128 × 128 | 5 × 5 µm² |
| 17 | 6 | G1 | 0 | 24 | 76 | exp3_0032 | exp3_0033 | 128 × 128 | 5 × 5 µm² |
| 18 | 78 | G10 | 0 | 96 | 4 | exp3_0034 | exp3_0035 | 128 × 128 | 5 × 5 µm² |
| 19 | 0 | A1 | 0 | 0 | 100 | exp3_0036 | exp3_0037 | 128 × 128 | 5 × 5 µm² |

Table S2. Evidence-grounded scientific basis for complementary PL and KPFM measurements. KPFM-derived contact-potential, surface-potential, and work-function observables describe electrostatic or energetic behavior, whereas steady-state PL intensity and PLQY describe emissive output and TRPL or carrier lifetime describes carrier kinetics. Relationships involving steady-state PL intensity are most directly relevant to the present PL peak-intensity comparison. PLQY relationships provide related optical context, whereas TRPL and carrier-lifetime relationships provide broader carrier-dynamics context because those measurements were not performed in the present study. Counts report 15 retained paired relationships from seven papers. Co-observation supports a complementary interpretation and does not establish a causal KPFM-to-PL pathway.

| KPFM observable class | PL-family observable class | Retained relationships | Evidence-grounded scientific claim | How the measurements are complementary | Relevance to the present experiment | Interpretation limit |
| --- | --- | --- | --- | --- | --- | --- |
| Contact potential difference | Carrier lifetime / TRPL | 4 | Interfacial-potential or electric-field changes co-occur with changes in carrier decay or extraction kinetics. | The pair connects an energetic/electrostatic change to its carrier-kinetic response in the same treatment comparison. | Relative dark/light surface-potential signals and relative ΔSP were measured. TRPL/carrier lifetime was not measured and is retained only as broader carrier-dynamics context. | Lifetime direction is context dependent: shorter decay can indicate faster extraction or stronger recombination. Co-observation is not causation. |
| Contact potential difference | PL intensity / PLQY | 4 | Interfacial-potential changes co-occur with changes in radiative emission yield or net non-radiative loss. | The pair tests whether energetic-interface modification is accompanied by a change in emissive quality. | Closest present-study analogue: relative dark/light surface-potential signals or relative ΔSP paired with steady-state PL peak intensity. PLQY was not measured. | PL intensity also depends on excitation, absorption, thickness, collection, and stack geometry. Co-observation is not causation. |
| Surface potential | Carrier lifetime / TRPL | 2 | Changes in the spatial surface-potential landscape co-occur with changes in carrier decay or extraction kinetics. | The pair links where electrostatic heterogeneity occurs to how long carriers persist or how rapidly they transfer. | Relative dark/light surface-potential signals and relative ΔSP were measured. TRPL/carrier lifetime was not measured and is retained only as broader carrier-dynamics context. | Spatial scales and sampled regions may differ, and lifetime direction remains mechanism dependent. Co-observation is not causation. |
| Surface potential | PL intensity / PLQY | 3 | Surface-potential magnitude or uniformity changes co-occur with changes in emission intensity, yield, or homogeneity. | The pair distinguishes electrostatic uniformity from emissive uniformity and tests whether both respond to the same treatment. | Closest present-study analogue: relative dark/light surface-potential signals or relative ΔSP paired with steady-state PL peak intensity. PLQY was not measured. | Matched fields of view are needed for a spatial claim; ensemble co-trends alone are not causal evidence. |
| Work function | Carrier lifetime / TRPL | 1 | Work-function or energy-level-alignment changes co-occur with changes in carrier-transfer or recombination kinetics. | The pair connects an energy-level-alignment measurement to a kinetic response relevant to charge transfer. | Broader context only: neither calibrated work function nor TRPL/carrier lifetime was measured. The present KPFM output is an uncalibrated relative surface-potential signal, not work function. | Absolute work function requires calibrated tip/sign conventions, and lifetime direction is architecture dependent. |
| Work function | PL intensity / PLQY | 1 | Work-function or energy-level-alignment changes co-occur with changes in radiative emission efficiency. | The pair tests whether energy-level tuning is accompanied by a measurable emissive response. | Steady-state PL peak intensity was measured, but PLQY and calibrated work function were not. The present uncalibrated relative surface-potential signal is not equivalent to work function. | Only one retained relationship supports this pairing, and the current experiment uses surface potential rather than calibrated work function. |

Table S3. Evidence-level records for retained KPFM–PL-family relationships. The table reports 15 retained relationships with the sample or intervention context, paired KPFM and PL-family observables, direct reported results, evidence-grounded claim, complementary interpretation, interpretation limit, evidence strength, and causal-status classification. Relationships involving steady-state PL intensity or PLQY are most relevant to the present optical comparison, whereas TRPL and carrier-lifetime relationships provide broader context. All retained relationships are classified as complementary-only and do not establish a causal KPFM-to-PL pathway.

| Relationship ID | Paper title | DOI | Intervention or comparison | KPFM observable and direct result | PL-family observable and direct result | Evidence-grounded claim | Complementary interpretation | Interpretation limit | Evidence strength | Causal status |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| R01 | Electron-donor/-acceptor ratio-guided molecular engineering for buried interface optimization in n-i-p perovskite solar cells | 10.20517/energymater.2025.183 | control to AA, ABA, and DBA | contact potential difference (CPD) increases sequentially | PLQY 5.51% (control), 10.76% (AA), 11.70% (ABA), and 12.52% (DBA) Steady-state PL intensity is the closest analogue measured here; PLQY was not measured. | Interfacial-potential changes co-occur with changes in radiative emission yield or net non-radiative loss. | The pair tests whether energetic-interface modification is accompanied by a change in emissive quality. | PL intensity also depends on excitation, absorption, thickness, collection, and stack geometry. Co-observation is not causation. | triangulated | complementary_only |
| R02 | Electron-donor/-acceptor ratio-guided molecular engineering for buried interface optimization in n-i-p perovskite solar cells | 10.20517/energymater.2025.183 | control to AA, ABA, and DBA | contact potential difference (CPD) increases sequentially | carrier lifetime (τavg) 162.00 ns (control), 139.66 ns (AA), 90.77 ns (ABA), and 3.35 ns (DBA) Broader carrier-dynamics context; not directly measured in the present study. | Interfacial-potential or electric-field changes co-occur with changes in carrier decay or extraction kinetics. | The pair connects an energetic/electrostatic change to its carrier-kinetic response in the same treatment comparison. | Lifetime direction is context dependent: shorter decay can indicate faster extraction or stronger recombination. Co-observation is not causation. | triangulated | complementary_only |
| R03 | Regioisomeric Effects on Enhancing p ‐Type Characteristics of Self‐Assembled Molecules in Inverted Perovskite Solar Cells | 10.1002/advs.202521518 | FTO/Me-4PACz, FTO/Me-4PACz/3,7-Br, and FTO/Me-4PACz/2,8-Br treatment series | mean contact potential difference (CPD) −0.768, −0.782, and −0.863 V, respectively | steady-state PL intensity Increased further after 3,7-Br or 2,8-Br treatment relative to the Me-4PACz control. Steady-state PL intensity is directly relevant to the present optical comparison. | Across the same treatment series, the more-negative mean CPD values after 3,7-Br and 2,8-Br treatment accompanied increased steady-state PL intensity. | KPFM reports treatment-dependent interfacial potential, while PL reports the emissive response of perovskite grown on the same treatment groups. | KPFM characterized the treated SAM surfaces, whereas PL used perovskite layers on the corresponding substrates. The treatment comparison is matched, but the measurement fields/specimens differ; co-observation is not causation. | triangulated | complementary_only |
| R04 | Regioisomeric Effects on Enhancing p ‐Type Characteristics of Self‐Assembled Molecules in Inverted Perovskite Solar Cells | 10.1002/advs.202521518 | FTO/Me-4PACz, FTO/Me-4PACz/3,7-Br, and FTO/Me-4PACz/2,8-Br films | contact potential difference (CPD) -0.768, -0.782, and -0.863 V respectively | carrier lifetime (τavg) 2951 ns (Me-4PACz control), 4080 ns (3,7-Br), and 4278 ns (2,8-Br) Broader carrier-dynamics context; not directly measured in the present study. | Interfacial-potential or electric-field changes co-occur with changes in carrier decay or extraction kinetics. | The pair connects an energetic/electrostatic change to its carrier-kinetic response in the same treatment comparison. | KPFM characterized the treated SAM surfaces, whereas PL used perovskite layers on the corresponding substrates. The treatment comparison is matched, but the measurement fields/specimens differ; co-observation is not causation. | triangulated | complementary_only |
| R05 | Regioisomeric Effects on Enhancing p ‐Type Characteristics of Self‐Assembled Molecules in Inverted Perovskite Solar Cells | 10.1002/advs.202521518 | FTO/Me-4PACz, FTO/Me-4PACz/3,7-Br, and FTO/Me-4PACz/2,8-Br treatment series | CPD-distribution full width at half maximum (FWHM) Decreased after 3,7-Br and 2,8-Br treatment. | steady-state PL intensity Increased further after 3,7-Br or 2,8-Br treatment relative to the Me-4PACz control. Steady-state PL intensity is directly relevant to the present optical comparison. | Narrower CPD distributions after 3,7-Br and 2,8-Br treatment accompanied increased PL intensity in the corresponding treatment groups. | CPD-distribution width reports energetic uniformity, while PL reports the emissive response to the same treatment series. | KPFM characterized the treated SAM surfaces, whereas PL used perovskite layers on the corresponding substrates. The treatment comparison is matched, but the measurement fields/specimens differ; co-observation is not causation. | triangulated | complementary_only |
| R06 | Pure 2D Perovskite Formation by Interfacial Engineering Yields a High Open‐Circuit Voltage beyond 1.28 V for 1.77‐eV Wide‐Bandgap Perovskite Solar Cells | 10.1002/advs.202203210 | PEABr post-treatment at 60 °C | CPD between GBs and GIs cannot be clearly distinguished | carrier lifetime (τavg) 659.18 ns (PEABr-60), versus 449.46 ns (control), 622.12 ns (PEABr-25), and 551.75 ns (PEABr-100) Broader carrier-dynamics context; not directly measured in the present study. | Interfacial-potential or electric-field changes co-occur with changes in carrier decay or extraction kinetics. | The pair connects an energetic/electrostatic change to its carrier-kinetic response in the same treatment comparison. | Lifetime direction is context dependent: shorter decay can indicate faster extraction or stronger recombination. Co-observation is not causation. | triangulated | complementary_only |
| R07 | Graded Heterojunction Improves Wide-Bandgap Perovskite for Highly Efficient 4-Terminal Perovskite/Silicon Tandem Solar Cells | 10.34133/research.0196 | WBG perovskite film with GHJ versus control without GHJ | contact potential difference (CPD) Larger for the GHJ film than for the control. | TRPL average carrier lifetime 231.12 ns (GHJ) versus 92.31 ns (control); PbI2-rich intermediate: 173.91 ns. Broader carrier-dynamics context; not directly measured in the present study. | The GHJ film showed a larger CPD and a longer average TRPL lifetime than the control film. | KPFM reports the treatment-dependent surface-potential shift, while TRPL reports carrier-decay kinetics for the same film series. | The measurements were performed on corresponding film groups, not a spatially registered field. Longer lifetime can reflect suppressed recombination but does not establish a causal CPD pathway. | triangulated | complementary_only |
| R09 | Modulating Perovskite Surface Energetics Through Tuneable Ferrocene Interlayers for High‐Performance Perovskite Solar Cells | 10.1002/anie.202424041 | unpassivated control, compound 1, and compound 2-treated perovskite films | KPFM-derived surface work function 4.77 eV (control); negligible change with compound 1; 4.68 eV with compound 2. | steady-state PL intensity Increased for compounds 1 and 2 relative to the control. Steady-state PL intensity is directly relevant to the present optical comparison. | Both Fc compounds increased steady-state PL intensity, whereas a substantial KPFM-derived work-function decrease occurred only with compound 2. | PL distinguishes the passivation-related emissive response from KPFM-derived work-function tuning across the same treatment series. | KPFM and luminescence measurements used corresponding treatment groups but separate specimens/geometries. Co-trending does not establish that the work-function change caused the luminescence response. | triangulated | complementary_only |
| R10 | Modulating Perovskite Surface Energetics Through Tuneable Ferrocene Interlayers for High‐Performance Perovskite Solar Cells | 10.1002/anie.202424041 | unpassivated control versus compound 2-treated perovskite films | CPD-distribution standard deviation 24.8 mV (control) and 11.3 mV (compound 2). | PL-mapping intensity and spatial distribution Compound 2 showed a substantial mean decrease and much-improved homogeneity relative to the control in C60-contacted stacks. | The strongest narrowing of the CPD distribution (compound 2) accompanied the strongest and most spatially uniform PL quenching at the perovskite/C60 interface. | KPFM maps energetic uniformity, while PL mapping reports the spatial uniformity of charge extraction for the same interlayer series. | The maps were not spatially registered. In the C60-contacted PL stack, lower PL was interpreted as stronger extraction rather than as poorer emissive quality; the association is noncausal. | triangulated | complementary_only |
| R11 | Modulating Perovskite Surface Energetics Through Tuneable Ferrocene Interlayers for High‐Performance Perovskite Solar Cells | 10.1002/anie.202424041 | unpassivated control, compound 1, and compound 2-treated perovskite films | KPFM-derived surface work function 4.77 eV (control); negligible change with compound 1; 4.68 eV with compound 2. | TRPL average carrier lifetime 1046 ns (control), 1175 ns (compound 1), and 1525 ns (compound 2) Broader carrier-dynamics context; not directly measured in the present study. | Both Fc compounds lengthened the average carrier lifetime, whereas a substantial KPFM-derived work-function decrease occurred only with compound 2. | TRPL reports passivation-related carrier decay, while KPFM-derived work function reports energetic tuning across the same treatment series. | KPFM and luminescence measurements used corresponding treatment groups but separate specimens/geometries. Co-trending does not establish that the work-function change caused the luminescence response. | triangulated | complementary_only |
| R12 | Room Temperature Ionic Liquid Capping Layer for High Efficiency FAPbI 3 Perovskite Solar Cells with Long‐Term Stability | 10.1002/advs.202400117 | FAPbI3 control, BAI RT, and BAAc RT-treated films | surface-potential variation Approximately 80 mV (control) versus 10 mV (BAAc RT); both RT treatments reduced heterogeneity. | PL-mapping intensity and spatial uniformity BAAc RT exceeded the control and BAI RT films and showed stronger emission with minimal fluctuation. | Surface-potential magnitude or uniformity changes co-occur with changes in emission intensity, yield, or homogeneity. | The pair distinguishes electrostatic uniformity from emissive uniformity and tests whether both respond to the same treatment. | Matched fields of view are needed for a spatial claim; ensemble co-trends alone are not causal evidence. | triangulated | complementary_only |
| R13 | Room Temperature Ionic Liquid Capping Layer for High Efficiency FAPbI 3 Perovskite Solar Cells with Long‐Term Stability | 10.1002/advs.202400117 | FAPbI3 control versus BAAc RT-treated films | surface-potential variation Approximately 80 mV (control) versus 10 mV (BAAc RT). | steady-state PL intensity The BAAc RT-treated film was nearly twice as intense as the control. Steady-state PL intensity is directly relevant to the present optical comparison. | Surface-potential magnitude or uniformity changes co-occur with changes in emission intensity, yield, or homogeneity. | The pair distinguishes electrostatic uniformity from emissive uniformity and tests whether both respond to the same treatment. | Matched fields of view are needed for a spatial claim; ensemble co-trends alone are not causal evidence. | triangulated | complementary_only |
| R14 | Room Temperature Ionic Liquid Capping Layer for High Efficiency FAPbI 3 Perovskite Solar Cells with Long‐Term Stability | 10.1002/advs.202400117 | FAPbI3 control, BAI RT, and BAAc RT treatment series | surface-potential variation Approximately 80 mV (control) versus 10 mV (BAAc RT); both RT treatments reduced heterogeneity. | interfacial TRPL average lifetime 12.85 ns (control/HTL), 7.19 ns (BAI RT/HTL), and 6.62 ns (BAAc RT/HTL) Broader carrier-dynamics context; not directly measured in the present study. | BAAc RT reduced surface-potential heterogeneity and yielded the shortest interfacial TRPL decay in the same treatment series. | KPFM reports treatment-dependent electrostatic uniformity, while interfacial TRPL reports extraction/recombination kinetics for corresponding treatment groups. | KPFM and TRPL used corresponding treatments but different sample stacks/geometries. Shorter interfacial TRPL can reflect faster extraction or recombination; the association is noncausal. | triangulated | complementary_only |
| R15 | Imidazole Post‐Treated Self‐Assembled Monolayers for Inverted Perovskite Solar Cells | 10.1002/advs.202518676 | control NiOx/Me-4PACz versus 4,5-DI and 4,5-D-2-MI-modified HTLs | surface-potential distribution Modified HTLs showed higher surface potential and a more uniform distribution. | steady-state PL intensity The 4,5-D-2-MI-treated perovskite film exhibited higher intensity. Steady-state PL intensity is directly relevant to the present optical comparison. | The modified HTL series showed higher and more uniform surface potential, while the 4,5-D-2-MI-treated film showed higher PL intensity. | The pair distinguishes electrostatic uniformity from emissive uniformity and tests whether both respond to the same treatment. | Matched fields of view are needed for a spatial claim; ensemble co-trends alone are not causal evidence. | triangulated | complementary_only |
| R16 | Imidazole Post‐Treated Self‐Assembled Monolayers for Inverted Perovskite Solar Cells | 10.1002/advs.202518676 | control NiOx/Me-4PACz versus 4,5-DI and 4,5-D-2-MI-modified HTLs | surface-potential distribution Modified HTLs showed higher surface potential and a more uniform distribution. | TRPL carrier lifetime Longer for the modified films, with the greatest enhancement for 4,5-D-2-MI. Broader carrier-dynamics context; not directly measured in the present study. | The modified HTL series showed higher and more uniform surface potential together with longer TRPL carrier lifetime. | The pair links where electrostatic heterogeneity occurs to how long carriers persist or how rapidly they transfer. | Spatial scales and sampled regions may differ, and lifetime direction remains mechanism dependent. Co-observation is not causation. | triangulated | complementary_only |

Table S4. Exploratory raw and composition-adjusted PL–photoKPFM association tests. The table reports Pearson and Spearman coefficients, bootstrap confidence intervals, leave-one-out sensitivity, partial correlations adjusted for nominal PEA and BDA precursor fractions, and Benjamini-Hochberg q-values for 36 exploratory comparisons. None survived multiplicity correction at q < 0.05. The analyses are descriptive and do not support a causal relationship between the PL and photoKPFM observables. PL-derived fitted emissive components, where included, are spectral-model outputs and should not be interpreted as structurally confirmed phase fractions.

| KPFM metric | PL metric | n | Pearson r | Pearson p | Pearson bootstrap 95% CI | Spearman ρ | Spearman p | Spearman BH q | Composition controls | Partial Spearman ρ | Partial Spearman p | Partial Spearman BH q | Leave-one-out Spearman range | Interpretation status |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ¦ΔSP¦ | Top-read PL peak intensity | 13 | 0.406 | 0.169 | [−0.179, 0.810] | 0.418 | 0.156 | 0.494 | Nominal PEA and BDA precursor fractions | −0.072 | 0.833 | 0.862 | [0.294, 0.545] | Exploratory; no causal claim supported |
| Dark relative surface potential | Top-read PL peak intensity | 13 | 0.047 | 0.880 | [−0.483, 0.587] | 0.220 | 0.471 | 0.749 | Nominal PEA and BDA precursor fractions | 0.485 | 0.130 | 0.390 | [0.091, 0.413] | Exploratory; no causal claim supported |
| Dark relative surface potential | Dominant PL peak wavelength | 13 | −0.290 | 0.336 | [−0.782, 0.264] | −0.431 | 0.142 | 0.494 | Nominal PEA and BDA precursor fractions | −0.426 | 0.192 | 0.406 | [−0.627, −0.319] | Exploratory; no causal claim supported |
| Dark relative surface potential | PL-fitted 3D/3D-like emissive fraction | 13 | −0.159 | 0.604 | [−0.767, 0.420] | −0.040 | 0.896 | 0.921 | Nominal PEA and BDA precursor fractions | 0.104 | 0.761 | 0.862 | [−0.235, 0.094] | Exploratory; no causal claim supported |
| Dark relative surface potential | PL-fitted low-n (n=1-4) emissive fraction | 13 | 0.099 | 0.748 | [−0.494, 0.626] | 0.058 | 0.851 | 0.901 | Nominal PEA and BDA precursor fractions | −0.099 | 0.773 | 0.862 | [−0.101, 0.232] | Exploratory; no causal claim supported |
| Dark relative surface potential | PL-fitted n=1-like/2D emissive fraction | 13 | −0.103 | 0.737 | [−0.619, 0.466] | −0.080 | 0.796 | 0.890 | Nominal PEA and BDA precursor fractions | −0.275 | 0.414 | 0.639 | [−0.243, 0.100] | Exploratory; no causal claim supported |
| Dark relative surface potential | PL-fitted n=2-like emissive fraction | 13 | 0.632 | 0.021 | [0.340, 0.869] | 0.684 | 0.010 | 0.289 | Nominal PEA and BDA precursor fractions | 0.681 | 0.021 | 0.208 | [0.570, 0.753] | Exploratory; no causal claim supported |
| Dark relative surface potential | PL-fitted n=3-like emissive fraction | 13 | 0.546 | 0.053 | [0.249, 0.846] | 0.617 | 0.025 | 0.289 | Nominal PEA and BDA precursor fractions | 0.601 | 0.051 | 0.260 | [0.520, 0.733] | Exploratory; no causal claim supported |
| Dark relative surface potential | PL-fitted n=4-like emissive fraction | 13 | 0.070 | 0.820 | [−0.255, 0.671] | 0.490 | 0.089 | 0.459 | Nominal PEA and BDA precursor fractions | 0.452 | 0.162 | 0.390 | [0.413, 0.661] | Exploratory; no causal claim supported |
| Dark relative surface potential | PL-fitted n≥5/high-n emissive fraction | 13 | 0.084 | 0.785 | [−0.390, 0.476] | 0.078 | 0.801 | 0.890 | Nominal PEA and BDA precursor fractions | 0.207 | 0.542 | 0.750 | [−0.094, 0.220] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | Top-read PL peak intensity | 13 | 0.171 | 0.576 | [−0.339, 0.649] | 0.286 | 0.344 | 0.676 | Nominal PEA and BDA precursor fractions | 0.524 | 0.098 | 0.354 | [0.175, 0.441] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | Dominant PL peak wavelength | 13 | −0.303 | 0.314 | [−0.794, 0.349] | −0.348 | 0.244 | 0.549 | Nominal PEA and BDA precursor fractions | −0.548 | 0.081 | 0.325 | [−0.592, −0.217] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | PL-fitted 3D/3D-like emissive fraction | 13 | −0.166 | 0.587 | [−0.801, 0.477] | −0.090 | 0.771 | 0.890 | Nominal PEA and BDA precursor fractions | −0.084 | 0.806 | 0.862 | [−0.336, 0.063] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | PL-fitted low-n (n=1-4) emissive fraction | 13 | 0.130 | 0.673 | [−0.506, 0.662] | 0.087 | 0.778 | 0.890 | Nominal PEA and BDA precursor fractions | 0.084 | 0.806 | 0.862 | [−0.067, 0.306] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | PL-fitted n=1-like/2D emissive fraction | 13 | −0.018 | 0.954 | [−0.578, 0.571] | 0.006 | 0.985 | 0.985 | Nominal PEA and BDA precursor fractions | −0.049 | 0.887 | 0.887 | [−0.134, 0.182] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | PL-fitted n=2-like emissive fraction | 13 | 0.579 | 0.038 | [0.251, 0.865] | 0.594 | 0.032 | 0.289 | Nominal PEA and BDA precursor fractions | 0.613 | 0.045 | 0.260 | [0.441, 0.698] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | PL-fitted n=3-like emissive fraction | 13 | 0.463 | 0.111 | [0.027, 0.791] | 0.439 | 0.134 | 0.494 | Nominal PEA and BDA precursor fractions | 0.462 | 0.153 | 0.390 | [0.291, 0.577] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | PL-fitted n=4-like emissive fraction | 13 | −0.066 | 0.831 | [−0.471, 0.663] | 0.242 | 0.426 | 0.749 | Nominal PEA and BDA precursor fractions | 0.268 | 0.426 | 0.639 | [0.119, 0.542] | Exploratory; no causal claim supported |
| Illuminated relative surface potential | PL-fitted n≥5/high-n emissive fraction | 13 | 0.016 | 0.959 | [−0.430, 0.478] | 0.072 | 0.816 | 0.890 | Nominal PEA and BDA precursor fractions | 0.100 | 0.769 | 0.862 | [−0.070, 0.242] | Exploratory; no causal claim supported |
| ¦ΔSP¦ | Dominant PL peak wavelength | 13 | 0.122 | 0.692 | [−0.334, 0.661] | 0.381 | 0.199 | 0.511 | Nominal PEA and BDA precursor fractions | 0.336 | 0.313 | 0.563 | [0.301, 0.563] | Exploratory; no causal claim supported |
| ¦ΔSP¦ | PL-fitted 3D/3D-like emissive fraction | 13 | 0.064 | 0.835 | [−0.501, 0.755] | −0.090 | 0.771 | 0.890 | Nominal PEA and BDA precursor fractions | −0.168 | 0.622 | 0.829 | [−0.194, 0.065] | Exploratory; no causal claim supported |
| ¦ΔSP¦ | PL-fitted low-n (n=1-4) emissive fraction | 13 | 0.086 | 0.779 | [−0.526, 0.609] | 0.116 | 0.706 | 0.890 | Nominal PEA and BDA precursor fractions | 0.247 | 0.465 | 0.669 | [−0.033, 0.228] | Exploratory; no causal claim supported |
| ¦ΔSP¦ | PL-fitted n=1-like/2D emissive fraction | 13 | 0.296 | 0.326 | [−0.320, 0.743] | 0.216 | 0.478 | 0.749 | Nominal PEA and BDA precursor fractions | 0.273 | 0.417 | 0.639 | [0.065, 0.337] | Exploratory; no causal claim supported |
| ¦ΔSP¦ | PL-fitted n=2-like emissive fraction | 13 | −0.433 | 0.139 | [−0.725, −0.167] | −0.372 | 0.211 | 0.511 | Nominal PEA and BDA precursor fractions | −0.571 | 0.066 | 0.298 | [−0.505, −0.274] | Exploratory; no causal claim supported |
| ¦ΔSP¦ | PL-fitted n=3-like emissive fraction | 13 | −0.491 | 0.089 | [−0.821, −0.221] | −0.608 | 0.028 | 0.289 | Nominal PEA and BDA precursor fractions | −0.710 | 0.014 | 0.208 | [−0.725, −0.566] | Exploratory; no causal claim supported |
| ¦ΔSP¦ | PL-fitted n=4-like emissive fraction | 13 | −0.284 | 0.347 | [−0.683, −0.062] | −0.409 | 0.165 | 0.494 | Nominal PEA and BDA precursor fractions | −0.386 | 0.241 | 0.481 | [−0.566, −0.349] | Exploratory; no causal claim supported |
| ¦ΔSP¦ | PL-fitted n≥5/high-n emissive fraction | 13 | −0.380 | 0.200 | [−0.716, 0.223] | −0.370 | 0.213 | 0.511 | Nominal PEA and BDA precursor fractions | −0.700 | 0.016 | 0.208 | [−0.459, −0.179] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | Top-read PL peak intensity | 13 | 0.464 | 0.111 | [−0.075, 0.823] | 0.462 | 0.112 | 0.494 | Nominal PEA and BDA precursor fractions | −0.095 | 0.781 | 0.862 | [0.350, 0.601] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | Dominant PL peak wavelength | 13 | 0.011 | 0.970 | [−0.486, 0.552] | 0.304 | 0.313 | 0.662 | Nominal PEA and BDA precursor fractions | 0.070 | 0.838 | 0.862 | [0.200, 0.493] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | PL-fitted 3D/3D-like emissive fraction | 13 | 0.007 | 0.983 | [−0.562, 0.582] | −0.124 | 0.686 | 0.890 | Nominal PEA and BDA precursor fractions | −0.316 | 0.344 | 0.590 | [−0.239, 0.022] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | PL-fitted low-n (n=1-4) emissive fraction | 13 | 0.095 | 0.758 | [−0.542, 0.608] | 0.116 | 0.706 | 0.890 | Nominal PEA and BDA precursor fractions | 0.336 | 0.312 | 0.563 | [−0.033, 0.236] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | PL-fitted n=1-like/2D emissive fraction | 13 | 0.346 | 0.246 | [−0.314, 0.787] | 0.279 | 0.357 | 0.676 | Nominal PEA and BDA precursor fractions | 0.494 | 0.122 | 0.390 | [0.134, 0.430] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | PL-fitted n=2-like emissive fraction | 13 | −0.333 | 0.266 | [−0.683, −0.020] | −0.234 | 0.441 | 0.749 | Nominal PEA and BDA precursor fractions | −0.430 | 0.187 | 0.406 | [−0.349, −0.183] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | PL-fitted n=3-like emissive fraction | 13 | −0.430 | 0.143 | [−0.797, −0.172] | −0.523 | 0.067 | 0.450 | Nominal PEA and BDA precursor fractions | −0.674 | 0.023 | 0.208 | [−0.678, −0.476] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | PL-fitted n=4-like emissive fraction | 13 | −0.530 | 0.063 | [−0.795, −0.184] | −0.510 | 0.075 | 0.450 | Nominal PEA and BDA precursor fractions | −0.604 | 0.049 | 0.260 | [−0.624, −0.340] | Exploratory; no causal claim supported |
| Signed ΔSP (light - dark) | PL-fitted n≥5/high-n emissive fraction | 13 | −0.276 | 0.362 | [−0.687, 0.325] | −0.167 | 0.585 | 0.877 | Nominal PEA and BDA precursor fractions | −0.471 | 0.143 | 0.390 | [−0.340, −0.055] | Exploratory; no causal claim supported |